## Slide 1
A.R. Farinha1, R. Mendes2 and M. T. Vieira1
1CEMUC® Group of Nanomaterials and Micromanufacturing
2ADAI– Association for the Development of Industrial Aerodynamics
Mechanical Engineering Department - University of Coimbra – Portugal
Austenitic stainless steel powders consolidated by explosive:
role of particle size in austenite content
XI International Symposium on Explosive Production of New Materials: Science, Technology,
Business and Innovations;
2-5 May 2012, Strasbourg, France

## Slide 2: Content
EPNM, 2012
Objective
Explosive compaction process
Explosive characteristics
Results
Conclusions

## Slide 3: Objective
Spherical austenitic stainless steel 316L powder
Size
Structure
Explosive consolidation behaviour
Ferrite
d50=28 m
d50=9 m
d50=5 m
Si
ze
EPNM, 2012

## Slide 4: Explosive densification: Process
Cylindrical Configuration
EPNM, 2012

## Slide 5: Explosive densification: Process
EPNM, 2012

## Slide 6: Explosive
  Emulsion Explosive – Ammonium nitrate based water-in-oil emulsion
  AN/water/wax, emulsifiers (84/10/6)
  Hollow perlite micro spheres (15 -10 %(w/w))
  Different detonation velocity (3.5 – 4.0 mm/s)
EPNM, 2012

## Slide 7
Explosive characterization
250 mm
EPNM, 2012

## Slide 8
Explosive – Detonation velocity
- The non-ideal behaviour of EX detonation process, is well-defined in the low porosity zone.
- D(r0) curves, Silvestrov model (2006)
EPNM, 2012

## Slide 9
Effect of phase transition on compact features
Powder:
Austenite
No cracks
Powder:
Austenite
Ferrite
Cracks
Powder:
Ferrite
Austenite
some Cracks
Detonation velocity = 3.5 mm/s; E/M= 1.1

## Slide 10
Powder:
Austenite
No cracks
Compact:
Austenite
Ferrite
Periphery Centre
Effect of phase transition on compact features
EPNM, 2012
Detonation velocity = 3.5 mm/s; E/M= 1.1

## Slide 11
Powder:
Austenite
Ferrite
Cracks
Compact periphery:
Austenite / Ferrite
Compact centre:
Austenite
Periphery Centre Periphery
Effect of phase transition on compact features
EPNM, 2012
Detonation velocity = 3.5 mm/s; E/M= 1.1

## Slide 12
Powder:
Ferrite
Austenite
Cracks
Compact:
Ferrite
Austenite
Effect of phase transition on compact features
EPNM, 2012
Detonation velocity = 3.5 mm/s; E/M= 1.1
Periphery Centre

## Slide 13
Powder:
Austenite
micro
Cracks
Powder:
Austenite
Ferrite
Cracks
Powder:
Ferrite
Austenite
Cracks
Detonation velocity = 4 mm/s; E/M= 1.3
Effect of phase transition on compact features

## Slide 14
Powder:
Austenite
Micro Cracks
Compact:
Austenite
Ferrite
Effect of phase transition on compact features
EPNM, 2012
Detonation velocity = 4 mm/s; E/M= 1.3
Periphery Centre

## Slide 15
Powder:
Austenite
Ferrite
Cracks
Compact periphery:
Austenite / Ferrite
Compact centre:
Austenite
Effect of phase transition on compact features
EPNM, 2012
Periphery Centre Periphery
Detonation velocity = 4 mm/s; E/M= 1.3

## Slide 16
Powder:
Ferrite
Austenite
Cracks
Compact periphery:
Ferrite / Austenite
Compact centre:
Austenite
Effect of phase transition on compact features
Periphery Centre Periphery
EPNM, 2012
Detonation velocity = 4 mm/s; E/M= 1.3

## Slide 17: Conclusion
The very fine powders subjected to high cooling rates, during atomisation process, present a considerable amount of ferrite, which was not the case for the large powder size.
The ferrite fraction underwent a phase transition to austenite (compact centre) when subject to a explosive compaction. A circular and radial cracks are generated.
On the contrary, larger powders subjected to the explosive compaction, exhibit a small fraction of ferrite after compaction. A good compacts were obtained.
EPNM, 2012

## Slide 18
Thank you for your attention
Ricardo Mendes
  ricardo.mendes@dem.uc.pt
  rita.farinha@dem.uc.pt
Acknowledgments
The authors would like to thank the Portuguese Foundation for Science and Technology (FCT) through SFRH/BD/41214/2007 for financial support, and to LEDAP –Lab. Energetics and Detonics