## Slide 1: Metastable, amorphous and quasicrystalline phases in explosively welded materials
I.A. Bataev, V.I. Mali, K. Hokamoto, H. Keno, M.A. Esikov, A.A. Bataev, A.V. Vinogradov and I.A. Balagansky
1. Novosibirsk State Technical University, Novosibirsk, Russia
2. Lavrent'ev Institute of Hydrodynamics, Siberian Branch, Russian Academy of Sciences, Novosibirsk, Russia
3. Shock Wave and Condensed Matter Research Center, Kumamoto University, Kumamoto , Japan

## Slide 2: Outline
1. “Classical” ways to vetrification of metals and alloys
2. Amorphization of metal at explosive welding of Ti and Al
3. Amorphization of metals at explosive welding of Nb and stainles steel
4. Formation of quasicristals at explosive welding of Ni and Al
5. Conclusions

## Slide 3: 1. “Classical” ways to vetrification of metals and alloys
1. Physical vapor deposition (i.e. magnetron sputtering)
2. Strain-induced amorphization (i.e. during mechanical alloying)
3. Rapid solidification of liquid phase.
“…non-crystalline structures can be obtained for some, perhaps all, metals and alloys by quenching rapidly enough from the molten state”. W. Klement, R.H. Willens. P. Duwez. Nature 187(1960)

## Slide 4: Rapid solidification of metals
Splat quenching
Melt spinning

## Slide 5: Bulk metallic glasses
Copper mold casting
Zr41.2Ti13.8Cu12.5Ni10.0Be22.5 – Vitreloy 1
Critical diameter is around 10 cm!!!

## Slide 6: Selection of amorphizable alloys composition
The empirical rules of Inoue*:
- multicomponent systems consisting of more than three elements;
- significant difference in atomic size ratios above about 12% among the three main constituent elements;
negative heats of mixing among the three main constituent elements;
most of the known glassy alloys compositions are located near deep eutectics
* Acta mater. 48 (2000) 279±306

## Slide 7: 2. Amorphization at welding of cpTi and Al-1%Mn
Typical composition of the vortex zone (wt %) | 
Ti | 35
Si | 0.2
Mn | 0.5
Al | Rest

## Slide 8: 2. Amorphization at welding of Ti and Al

## Slide 9: HRTEM of partially crystalline zone
Original image
FFT
Filtered FFT

## Slide 10: Elemental composition of amorphous phase (EDX results)
Ti, at % | Al, at%
37.6 | 62.4
The difference between rTi and rAl is only 2,7 %.
However the mixing enthalpy is -30 kJ/mol

## Slide 11: 2. Amorphization at underwater welding of Nb foil and stainless steel SUS304 plate*
SUS 304 composition | 
C | 0.08
Mn | 2.0
Si | 0.75
Cr | 18-20
Ni | 10.5
*experiments were carried out in collaboration with professor K. Hokamoto

## Slide 12: Nb-stainless steel interface

## Slide 13: Interface of Nb-SS explosively welded bimetal
Nb
SS
Zone of
mixing

## Slide 14: Glassy and partially crystalline parts of the interface
 | Cr | Fe | Ni | Nb
Wt % | 8.6 | 35.7 | 4.8 | 51.0
At % | 11.5 | 44.6 | 5.7 | 38.3

## Slide 15: Phase diagram analysis
- Eutectic point
- Expetimental ratio of the elements

## Slide 16: Precipitations in the mixing zone
(12-fold quasicristals?)
 | Cr | Ni | Nb | Mn | Fe
Wt % | 13,4 | 4,9 | 21,8 | 0,7 | Rest
At % | 15,6 | 5,1 | 14,3 | 0,8 | Rest

## Slide 17: Atomic radii and enthalpy of mixing analysis
 | Fe | Ni | Cr | Nb
Fe | - | 0,8% | 2,3% | 15,9%
Ni |  | - | 3,2% | 16,8%
Cr |  |  | - | 13,1%
Nb |  |  |  | -
 | Fe | Ni | Cr | Nb
Fe | - | -2 | -1 | -16
Ni |  | - | -7 | -30
Cr |  |  | - | -7
Nb |  |  |  | -
Atomic radii difference
Enthalpy of mixing (kJ/mol)
Correspond to Inoue’s rules
Contradict Inoue’s rules

## Slide 18: Simulation of Nb and flyer plate acceleration (step 1)*
* In collaboration with prof. I.A. Balagansky

## Slide 19: Simulation of Nb and SS collision (step 2)

## Slide 20: Distribution of pressure and temperature near the contact point
Calculated cooling rate is ~109 K/s

## Slide 21: 4. Formation of quasicristals at explosive welding of Ni and Al

## Slide 22: Decagonal quasicrystals in the mixing zone
HRTEM of decagonal phase
processed FFT
HRTEM FFT filtered image indicating local atomic arrangements with 10-fold symmetry
HRTEM

## Slide 23: Inoue’s rule analysis for Ni-Al system
The difference between rNi and rAl is 14,4 %.
The mixing enthalpy is -22 kJ/mol

## Slide 24: XRD pattern of the interface between Ni and Al plates

## Slide 25: Conclusions
Formation of amorphous, quasicrystalline and other metastable phases during explosive welding is highly probable
Due to high cooling rates explosive welding can be considered as one of rapid solidification techniques
However in contrast to rapid solidification techniques (e.g. melt spinning) the local conditions for different zones of melted metal are very nonuniform. Variation of concentration and effect of pressure have to be considered when describing a model of solidification. In the same time this variations open new approach to formation of metastable phases.

## Slide 26: Acknowledgements
Ivan Bataev gratefully acknowledge:
professor K. Hokamoto and his group for fruitful collaboration in welding of Nb and stainless steel
professor V.I. Mali and his group for help in experiments with Ti and Al explosive welding and Ni and Al explosive welding
colleagues of Materials Science Department of NSTU for useful discussions

## Slide 27
Thank you for your attention!

## Slide 28: Reported data on quasicrystals or amorphous phase formation at explosive welding
System | Amorphous/quasicrystals | Reference
Ti-Al | Amourphous | This study
Ni-Al | Quasicrystals | This study
Nb-Stainless steel | Amorphous +QC precipitaions | This study
Ti-Steel (0,09% C) | Amorphous | Chiba et al. Materials Science Forum Vols. 465-466 (2004) pp 465-474 M. Nishida, A. Chiba, Mater. Trans. JIM 36 (11)
Ti-Ni | Amorphous and icosahedral QC | Chiba et al. Materials Science Forum Vols. 465-466 (2004) pp 465-474 M. Nishida, A. Chiba, Mater. Trans. JIM 36 (11)
Zr-Steel | Amorphous | H.Paul et al. EPNM2014 abstract