## Slide 1: CARRYING ON MEZHANOV'S TRADITIONS: NEW ACHIEVEMENTS ON SHS IN ISMAN
M.I.Alymov, I.P.Borovinskaya, A.S. Rogachev

## Slide 2: Plan of the lecture
Development of combustion science
  Macroscopic theory and experiments
  Microscopic models
Macro- micro- and nano-structured SHS systems
Product structure formation and design
Applications and commercialization

## Slide 3
http://z-walls.ru/oboi/siluet_alpinist_chelovek_gory_sneg
Theory
Trial-and-error
Experiment
Tradition #1: Don’t miss theory

## Slide 4: SHS and Combustion Theory
“Up to now, structure-macro-kinetic theory of SHS that consider the combustion process together with structure-formation … has not been created”
“Possibility for development of generalized theory of flame propagation in heterogeneous media, that is important not only for SHS, has appeared”
(A.G.Merzhanov, I.P.Borovinskaya, “Concept of SHS development”, Chernogolovka, 2003)

## Slide 5: New phenomena in filtration combustion
Reaction spots and fingering (Ti – Air)
Laboratory of Prof. Petr M.Krishenik
Kostin, S.V., Krishenik, P.M., and Shkadinsky, K.G.,Experimental study of the heterogeneous filtration combustion mode, Combust. Explos. Shock Waves, 2012, vol. 48, no. 1, pp. 1–9.
Kostin, S.V. and Krishenik, P.M., Unsteady infiltration mediated combustion in conditions of regulated quasiisobaric flow of gaseous reagent, Int. J. Self. Propag. HighTemp. Synth., 2013, vol. 22, no. 2, pp. 88–92.

## Slide 6: New phenomena in filtration combustion
Computer modeling
Ozerkovskaya, N.I., Firsov, A.N., and Shkadinsky, K.G., Emergence of spatial structures during filtration combustion, Combust. Explos. Shock Waves, 2010, vol. 46, no. 5, pp. 515–522.
Kostin, S.V., Krishenik, P.M., Ozerkovskaya, N.I., Firsov, A.N., and Shkadinsky, K.G., Cellular filtration combustion of porous layers, Combust.Explos. Shock Waves, 2012, vol. 48, no. 1, pp. 1–9.
Laboratory of Prof. Petr M.Krishenik

## Slide 7
Combustion of powder and granulated Ti+0.5C
3 mm/s
9 mm/s
Laboratory of Dr. Boris S. Seplyarskii

## Slide 8
Combustion of granulated Ti+0,5C: yield
Laboratory of Dr. Boris S. Seplyarskii
Combustion in Ar: carbide
Combustion in N2: carbonitride
Contribution to combustion science
New SHS products
New SHS products

## Slide 9: High speed Macro- and Micro- video: influence of the medium microstructure
Ni+Al Mechanically structured System
Ti+B System

## Slide 10: Dynamics of the local combustion front movement

## Slide 11: 2D model of the microheterogeneous combustion and experimental verification
P.M.Krishenik, K.G.Shkadinskii, S.A.Rogachev, 2013
Laboratory of Prof. Petr M.Krishenik

## Slide 12: mutual contributions of shs and combustion science (made recently)
New regimes of combustion wave propagation, fingering
Microstructure and particles contacts as governing parameters for propagating velocity, discrete model of combustion
Correlations between combustion mechanisms and microstructure of solid products

## Slide 13: Merzhavov’s traditions
Tradition #2: Develop new methods of experimental diagnostics
Tradition #3: Study structure formation processes
Tradition #4: Create new materials and structures
Tradition #5: Cover the whole way from fundamental idea to applications

## Slide 14: Probing local gas pressure during SHS
Dr. Sergey G. Vadchenko, Alexander S. Schukin
Ti-C system

## Slide 15: Voltage generated by shs under pressure
(1) Ti + B sample, (2) WR5/20 thermocouples,
(3) igniting tablet, (4) igniting coil, (5) punch,
(6) heat insulator (sand), (7) mold,
(8) amplifier, (9) AD converter, and (10) PC.
P
Electromotive force (EMF) curves recorded during combustion of Ti-B mixture with ratio B/Ti = 0,75
Prof. Vladimir A. Scherbakov, Dr. Valeryi N. Barinov

## Slide 16
spectrums
ACOUSTIC DIAGNOSTICS OF ORGANIC SHS
acoustic emission
t, (μs)
f, (kHz)
acoustic signal
autocorrelation function (ACF)
ACF
ACF
Fourier-spectra of ACF
FSACF(x10-3)
C4H10N2 + R(COOH)2n  C4H10N2 · R(COOH)2n + Q
Dr. Evgenii G. Klimchyk

## Slide 17
TR-XRD of combustion 3TiSi2C mixture
Initial mixture
Product
Ti3SiC2
Ti3SiC2
Ti3SiC2
Laboratories of Dr. Alexander E. Sytschev and Dr. Dmitry Yu. Kovalev
Hunting for MAX-phases: I

## Slide 18
Hunting for MAX-phases: II
Laboratoriy of Dr. Alexander E. Sytschev

## Slide 19
Hunting for MAX-phases: III
Ti3SiC2
TiC
TEM HR
In collaboration with Notre Dame University

## Slide 20
Ti
Ti
Ti
Ti, Al
Ti2AlC
Т, 0С
Time, s
2θ, deg.
28
42
49
35
56
63
Ti
Ti
Ti
Ti, Al
Al
Ti2AlC
C
C
B
A
Ti2AlC
2θ, deg.
Ti2AlC
Ti2AlC
TiAl
TiAl
TiAl
Al
Ti2AlC
Ti2AlC
Ti2AlC
Ti2AlC
TiAl
TiAl
A
B
TiAl
TiAl
Combustion of the Ti-Al-C mixture in the helium: TRXRD picture and thermogram of process
Laboratoriy of Dr. Dmitry Yu. Kovalev

## Slide 21
Preparation of Ti2AlN by Reactive Sintering
Point | Ti | Al | N
1 | 67.43 | 23.30 | 9.27
2 | 68.24 | 21.57 | 10.19
Way, which provides output target product Ti2AlN not less than 99% - isothermal annealing in argon (0.3 MPa) at temperatures 13000C during 2 hour.
Laboratories of Dr. Alexander E. Sytschev and Dr. Dmitry Yu. Kovalev
Hunting for MAX-phases: IV

## Slide 22: New materials: alon
Borovinskaya I.P., Ignat’eva T.I., Semenova V.N., and Chemagina E.A. SHS of Aluminum Oxynitride in Chemical Furnace. Int. J. SHS, 2015, Vol. 24, No. 4.
Conjugated reactions (chemical oven)
2B + N2 = 2BN - heat source and secondary product
Al + 2Al2O3 + N2 = 2Al5O6N – primary product

## Slide 23: New morphologies: si3n4
Borovinskaya I.P., Loryan V.E., and Zakorzhevsky V.V. In: Nitride Ceramics: Combustion Synthesis, Properties, and Applications. Wiley-VCH Verlag GmbH, 2014, pp. 1-49.
b – Si3N4
Modified morpholody with fusing agent

## Slide 24: New microstructures: submicron and nano- powders
BN
MoSi2
WC
Боровинская И.П., Игнатьева Т.И., Вершинников В.И., и др. Технология СВС наноразмерных порошков тугоплавких соединений. Российские нанотехнологии, 2007, т. 2, с.114-119.

## Slide 25: New chemical route: B + co2
Reaction mechanism
В + СО2  В2О3 + СО
В2О3 (ж) + 3.44С(тв) = В4С + газовая фаза (В2О2, ВО2, ВО)
2В2О2 (г) + 6СО(г) = В4С(тв) + 5СО2 (г)
2В2О2 (г) + 8СО(г) = В4С(тв) + 7СО2 (г)
2В2О2 (г) + 5СО(тв) = В4С(тв) + СО

## Slide 26
I.P.Borovinskaya, E.A.Chemagina, T.I.Ignatyeva, - work in progress
Whiskers and nanotube produced by combustion of B with CO2

## Slide 27
Green
mixture
Combustion
Phase segregation
of melt products
Solidification
and cooling
Oxide
(Al2O3)
Cast alloy
Centrifugal
acceleration
(n = a/g)
Centrifugal SHS of multicomponent alloys
(M1 + M2 + M3 + ... + Mn) + (N1 + N2 + ... + Nn) + R  [CAs] +Al2O3 + Q
where Mn stands for oxides of Cr, Ni, Co, Nb, W, Mo, Mn, etc.; Nn stands for nonmetals such as C, B, etc.; and R is reducing agent (Al); CAs cast alloys;
Q heat release.
Laboratory of Prof. Vladimir I. Yukhvid

## Slide 28
New materials: high-entropy NiCrCoFeMnAlx alloys by SHS-casting
After light etching (SEM)
X=2
Vladimir Sanin*, Denis Ikornikov, Dmitry Andreev, Vladimir Yukhvid

## Slide 29: POLYMETALLIC CATALYSTS ON THE BASE OF SHS-INTERMETALLIDES
Complex multicomponent intermetallides (aluminides) produced in one-stage short-term SHS were the precursors for new class of catalysts.
The catalysts were produced by leaching and stabilizing of intermetallic alloys.
The catalysts composition consisted of iron group metals (Fe, Ni, Co) as main components with addition of other d-metals and rare-earth elements (V, Mn, Cu, Zr, Mo, La, Ce etc.) as promoters. Catalysts demonstrated high activity and selectivity both in oxidative and in reducing processes.
The catalysts are composite materials in fact, with highly disordered nanostructured metal-oxide phases supported by unleached phases of lower intermetallides.
The catalysts surface was covered by two-level nanostructures. Low-level structures observed for all catalysts samples and consisted of almost perfect or slightly distorted plane hexagons of 1-2 mm in diameter and 10 - 100 nm in thickness. Inner structure of these hexagons depended on chemical composition and consists of 10-30 nm granules or fine unresolved substructures.
We suppose the nanostructures noted are main reason of high catalytic properties of these materials.
Laboratory of Dr. Vyacheslav N. Borsch

## Slide 30: NANOSTRUCTURES OF Ni- AND Fe-BASED CATALYSTS OF DEEP OXIDATION
85Ni-10Co-5Mn
2 mm
79Fe-15Co-6Mn
2 mm
90Fe-5Mn-5Ce
2 mm
200 nm
79Fe-15Co-6Mn
Laboratory of Dr. Vyacheslav N. Borsch

## Slide 31: DEEP OXIDATION OF CO AND PROPANE ON Ni-Co-Mn CATALYSTS
Propane conversion, %
CO conversion, %
Temperature, 0C
Temperature, 0C
V.N.Borshch, E.V.Pugacheva, S.Ya.Zhuk, D.E.Andreev, V.N.Sanin, V.I.Yukhvid / Doklady Physical Chemistry, 2008, Vol.419. Part 2, pp.77-79.
V.N.Sanin, D.E.Andreev, E.V.Pugacheva, S.Ya.Zhuk, V.N.Borshch, V.I.Yukhvid / Inorganic Materials, 2009, Vol.45, No.7, pp.777-784
E.V.Pugacheva, V.N.Borshch, S.Ya.Zhuk, D.E.Andreev, V.N.Sanin, V.I.Yukhvid. / Int. J. SHS, 2010, V.19, No.1, pp. 65–69.
Laboratory of Dr. Vyacheslav N. Borsch

## Slide 32: NANOSTRUCTURES ON THE SURFACE OF Co-BASED CATALYSTS FOR FISCHER-TROPSCH PROCESS
100 nm
40 nm
95Co-5Ce
95Co-5Ce-5Zr
95Co-5Ce-5Zr
200 nm
20 nm

## Slide 33: ACTIVITY AND SELECTIVITY OF Co-BASED CATALYSTS IN FISCHER-TROPSCH PROCESS P=2.0 MPa, t=2000C, H2:CO = 2:1, V=2.5 l(NTP)Ч(sЧg)-1
Catalyst | Activity, (mmol CO)Ч (sЧg)-1 | Selectivity, %mol |  |  | Compound of C5+ products | 
 |  | CH4 | C5+ | CO2 | ASF a | iso- / n-
Co | 1.29 | 7.2 | 92.8 | 0.0 | 0.90 | 0.18
50Co-50Ni | 2.11 | 6.7 | 92.6 | 0.5 | 0.91 | 0.15
95Co-5V | 1.27 | 7.1 | 92.9 | 0.0 | 0.92 | 0.16
95Co-5Zr | 0.97 | 7.5 | 91.8 | 0.0 | 0.91 | 0.17
95Co-5Ce | 4.64 | 12.7 | 73.7 | 1.1 | 0.82 | 0.15
95Co-5La | 3.37 | 4.0 | 93.8 | 1.1 | 0.94 | 0.13
90Co-5Ce-5Zr | 2.63 | 12.3 | 82.0 | 2.0 | 0.85 | 0.14
90Co-5La-5Zr | 3.24 | 8.0 | 87.6 | 1.4 | 0.88 | 0.16
20Co-0.5Re/Al2O3 | 3.95 | 7.0 | 88.0 | 1.5 | 0.83 | 0.25
V.N.Borshch, O.L.Eliseev, S.Ya.Zhuk, R.V.Kazantsev, D.E.Andreev, V.N.Sanin, V.I.Yukhvid and A.L.Lapidus / Doklady Physical Chemistry, 2013, Vol.451. Part 2, pp.167-171.
V.N.Borshch, E.V.Pugacheva, S.Ya.Zhuk, D.E.Andreev, V.N.Sanin, V.I.Yukhvid O.L.Eliseev, R.V.Kazantsev, S.I.Kolesnikov, I.M.Kolesnikov,and A.L.Lapidus / Kinetics and Catalysis, 2015, Vol.56, No.5, pp.681-688.
Laboratory of Dr. Vyacheslav N. Borsch

## Slide 34: Mo-Ni-CATALYSTS OF HYDRODESULPHURIZATION PROCESS (hydropurification of diesel fraction)
Catalyst | Initial concentration of total sulphur in diesel fraction, ppm | Residual sulphur concentration, ppm |  | 
 |  | 2500С | 3500С | 4000С
АNМ-1 | 9900 | 7200 | 33 | 288
АNМ-2 | 9900 | 7230 | 37 | 312
АNМ-3 | 9900 | 7410 | 45 | 335
АNМ-4 | 9900 | 7490 | 52 | 358
V.N.Borshch, E.V.Pugacheva, S.Ya.Zhuk, D.E.Andreev, V.N.Sanin, V.I.Yukhvid O.L.Eliseev, R.V.Kazantsev, S.I.Kolesnikov, I.M.Kolesnikov,and A.L.Lapidus / Kinetics and Catalysis, 2015, Vol.56, No.5, pp.681-688.

## Slide 35: Cold rolling of Reactive films with corrugated (profiled) surface
20 mm
Q ~ 1200 – 1300 J/g
dQ/dt ~ 1 MJ/g s
Dr. Sergey G, Vadchenko
TiB2

## Slide 36: Ceramic items produced by SHS
Prof. I.P.Borovinskaya with co-workers

## Slide 37: SHS in space: ISS

## Slide 38: SHS in space: unmanned spacecraft
Dr. A.E.Sytschev, S.G.Vadchenko, et al.

## Slide 39: Wave of CuTi(amorph) to CuTi (cryst) transformation
- Distance, mm
2 θ
Distance, mm
Intensity of
XRD peak, counts
CuTi
CuTi
CuTi(amorphous) CuTi (crystalline intermetallic)

## Slide 40: Some other achievements:
Production of ultrafine Ti through SHS hydrogenation-milling-furnace dehydrogenation route
New modification of boron carbide B25C4Mg1.42
Electric insulating ceramics BN-SiO2
Filters and membranes of TiC with catalytic activity
And others…

## Slide 41
Thank you for your attention!
Carrying on Merzhanov’s traditions…